## Slide 2: Accelerating FFF Printing via Viscous Heating
EXPERIMENTAL FINDINGS AND PREDICTIVE ALGORITHMS
Tim A. Osswald
Allen Jonathan Román

## Slide 3: Completed workflow
Experiments conducted to date:
Experimental Condition | Values Tested
Force [N] | 15.45
RPM [-] | 0, 2500, 5000, 7500
Temperature [C] | 265, 280, 295
Diameter [mm] | 3.175, 4.6725, 6.35
Material [-] | PA
Experimental Condition | Values Tested
Force [N] | 15.45
RPM [-] | 0, 2500, 5000, 7500
 | 265, 280, 295
Diameter [mm] | 3.175, 4.6725, 6.35
Material [-] | PA
Upcoming experiments will include varying force and higher RPMs
Future experiments will include testing on PEEK
Analysis workflow:
Response Surface Methodology algorithm has been implemented to analyze influences and predict future outcomes (=0.96)
Machine learning will also be implemented to predict future outcomes

## Slide 4: Response Surface Method – Pareto Chart
The magnitude of the standardized effects explains which coefficients have the most influence on the response, melting behavior.
Anything to the right of the red line is statistically significant
Pareto Summary:
Rank of input influences
  RPM > Diameter > Temperature
The interacting influence of Diameter-RPM is highly influential
Coefficient Summary:
Coefficients in green agree with Pareto analysis
  RPM > Diameter > Temperature

## Slide 5: Response Surface Method – Contour Plots
Contour plots can be made for experimental conditions to predict outcomes
Contour Plots Summary:
Melting rate is influenced much more as you increase RPM, depicted by the change in counter slopes
Prediction accuracy:
0 RPM
5000 RPM
10,000 RPM

## Slide 6: Response Surface Method – Conclusions
For the initial tests, it shows statistically that heater temperature can be reduced and an increase in RPM would be able to compensate and increase melting rate.
225 melting rate can be reached with the following conditions
0 RPM @ 295C
1500 RPM @ 280C
3000 RPM @ 265C
Diameter = 4.6725 mm

## Slide 7: Influence of Filament Diameter on Viscous Heating
Diameter = 4.6725 mm
Diameter = 6.35 mm

## Slide 8: Influence of Filament Diameter on Viscous Heating
Normalized
Diameter = 4.6725 mm

## Slide 9: Influence of Filament Diameter on Viscous Heating
Normalized
Diameter = 6.35 mm

## Slide 10: Influence of Temperature on Viscous Heating
280C
295C

## Slide 11: Influence of Temperature on Viscous Heating
Normalized
265C

## Slide 12: Accelerating FFF Printing via Viscous Heating
PROTOTYPE DESIGN WORK
Tim A. Osswald
Allen Jonathan Román

## Slide 13: Preliminary Prototype Design

## Slide 14: Crucial Dimensions of Prototype
Crucial dimensions which will be tested to ensure material flows properly
g [mm]= amount of filament exposed to direct heat
d [mm] = die length
  Longer die length to ensure relaxation occurs
r [mm] = radius
[degrees] = interior taper angle
[degrees]
d [mm]
g [mm]
r [mm]

## Slide 15: Crucial Dimensions of Prototype
Crucial dimensions which will be tested to ensure material flows properly
Issues to avoid with solutions:
Centrifugal forces to not allow proper extrusion
  Possible solution: Area highlighted in green will be threaded to act as a conveying screw. Additionally, guide tube will be counter-rotating to create positive pressure zone to ensure material does not go up.
Material will not have enough time to relax, resulting in extrusion defects
  Possible solution: Test various capillary lengths to ensure smooth extrudate
[degrees]
d [mm]
g [mm]
r [mm]

## Slide 17: Medium Diameter

## Slide 18: Medium Diameter

## Slide 19: Medium Diameter